# Text boxes

BUFFING

WHEEL

Direction

of Rotation

CUT

CUT MOTION

Gives you SMOOTH SURFACE,

SEMI-BRIGHT and UNIFORM.

The piece being polished should be moved

AGAINST the direction of the wheel, using

a medium to hard pressure.

COLOR MOTION

Gives you BRIGHT, SHINY,

and CLEAN SURFACE.

The piece being polished should be moved

TOWARD the direction of the wheel, using

a medium to light pressure.

COLOR

Direction

of Rotation

BUFFING

WHEEL

For best results, your buffing wheel should maintain a surface speed of between

3600 and 7500 Surface Feet Per Minute (SFPM).  The higher your speed, the

better and quicker your results.

Calculating surface speed of wheel in SFPM.

SFPM = 1/4 x diameter of wheel x RPM (revolutions of spindle per minute)

Therefore an 8" wheel @ 3600 rpm = 2 x 3600 = 7200 SFPM

Eliminating ‘swirl’ marks

Swirl marks caused by buffing in the final stages can be easily removed by wetting the part with a damp cloth, then dusting with a powder, such as whiting, talcum powder or cornstarch. Then buff on your wheel again until the swirls disappear.